## Slide 1: Module 3
CARRIER TRANSPORT MECHANISM
Charge Carriers in semi-conductors
Drift and Diffusion of carriers
Mobility
Generation
Recombination and Injection of Carriers
Carrier Transport Equations
Excess Carrier Lifetime

## Slide 2: Mobile Charge Carriers in Semiconductors
Three primary types of carrier action occur inside a semiconductor:
  Drift: charged particle motion under the influence of an electric field.
  Diffusion: particle motion due to concentration gradient or temperature gradient.
  Recombination-generation (R-G)

## Slide 3: Electrons as Moving Particles
F = (-q)E = moa
F = (-q)E = mn*a
where mn* is the
conductivity effective mass
In vacuum
In semiconductor

## Slide 4: Conductivity Effective Mass, m*
Under the influence of an electric field (E-field), an electron or a hole is accelerated:
electrons
holes
 | Si | Ge | GaAs
mn*/mo | 0.26 | 0.12 | 0.068
mp*/mo | 0.39 | 0.30 | 0.50
mo = 9.110-31 kg
Electron and hole conductivity effective masses

## Slide 5: Carrier Scattering
Mobile electrons and atoms in the Si lattice are always in random thermal motion.
  Electrons make frequent collisions with the vibrating atoms
    “lattice scattering” or “phonon scattering” – increases with increasing T
Other scattering mechanisms:
  deflection by ionized impurity atoms
  deflection due to Coulombic force between carriers
    “carrier-carrier scattering” – only significant at high carrier concentrations
The net current in any direction is zero,
if no E-field is applied.
1
2
3
4
5
electron

## Slide 6: Thermal Velocity, vth
Average electron kinetic energy

## Slide 7: Carrier Drift
When an electric field (e.g. due to an externally applied voltage) exists within a semiconductor, mobile charge carriers will be accelerated by the electrostatic force:
1
2
3
4
5
electron
E
Electrons drift in the direction opposite to the E-field  net current
Because of scattering, electrons in a semiconductor do not undergo constant acceleration. However, they can be viewed as quasi-classical particles moving at a constant average drift velocity vdn

## Slide 8: Carrier Drift (Band Model)
Ec
Ev

## Slide 9: Electron Momentum
With every collision, the electron loses momentum
Between collisions, the electron gains momentum
–q E tmn
  tmn ≡ average time between electron scattering events
Conservation of momentum 
|mn*vdn | = | q E tmn|

## Slide 10: Carrier Mobility m
|vdn| = qEtmn / mn* ≡ mnE
n  [qtmn / mn*] is the electron mobility
p  [qtmp / mp*] is the hole mobility
Similarly, for holes:
|vdp|= qEtmp / mp*  mpE
 | Si | Ge | GaAs | InAs
mn (cm2/Vs) | 1400 | 3900 | 8500 | 30,000
mp (cm2/Vs) | 470 | 1900 | 400 | 500
Electron and hole mobilities for intrinsic semiconductors @ 300K
For electrons:

## Slide 11: Example: Drift Velocity Calculation
a) Find the hole drift velocity in an intrinsic Si sample for E = 103 V/cm.
b) What is the average hole scattering time?
vdp = mpE
Solution:
a)
b)

## Slide 12: Mean Free Path
Average distance traveled between collisions

## Slide 13: Mechanisms of Carrier Scattering
Dominant scattering mechanisms:
  1. Phonon scattering (lattice scattering)
  2. Impurity (dopant) ion scattering
Phonon scattering limited mobility decreases with increasing T:
 = q / m

## Slide 14: Impurity Ion Scattering
There is less change in the electron’s direction if the electron travels by the ion at a higher speed.
Ion scattering limited mobility increases with increasing T:

## Slide 15: Matthiessen's Rule
 Probability that a carrier will be scattered by any mechanism within a time period dt is
The probability that a carrier will be scattered by mechanism i within a time period dt is
  ti ≡ mean time between scattering events due to mechanism i

## Slide 16: Mobility Dependence on Doping
Carrier mobilities in Si at 300K

## Slide 17: Mobility Dependence on Temperature

## Slide 18: Hole Drift Current Density Jp,drift
vdp Dt A = volume from which all holes cross plane in time Dt
p vdp Dt A = number of holes crossing plane in time Dt
q p vdp Dt A = hole charge crossing plane in time Dt
q p vdp A = hole charge crossing plane per unit time = hole current
 Hole drift current per unit area Jp,drift = q p vdp

## Slide 19: Conductivity and Resistivity
In a semiconductor, both electrons and holes conduct current:
The conductivity of a semiconductor is
  Unit: mho/cm
The resistivity of a semiconductor is
  Unit: ohm-cm

## Slide 20: Resistivity Dependence on Doping
n-type
p-type
Lecture 4, Slide 20
For n-type material:
For p-type material:
Note: This plot (for Si) does not apply to compensated material (doped with both acceptors and donors).

## Slide 21: Electrical Resistance
where r is the resistivity
Resistance
[Unit: ohms]
V
+
_
L
t
W
I
uniformly doped semiconductor

## Slide 22: Example: Resistance Calculation
What is the resistivity of a Si sample doped with 1016/cm3 Boron?
Answer:

## Slide 23: Example: Dopant Compensation
Consider the same Si sample doped with 1016/cm3 Boron, and additionally doped with 1017/cm3 Arsenic. What is its resistivity?
Answer:
(1017-1016)

## Slide 24: Example: T Dependence of r
Consider a Si sample doped with 1017cm-3 As. How will its resistivity change when the temperature is increased from T=300K to T=400K?
Answer:
The temperature dependent factor in  (and therefore ) is n.
From the mobility vs. temperature curve for 1017 cm-3, we find that n decreases from 770 at 300K to 400 at 400K.
Thus,  increases by

## Slide 25: Summary of Charge carriers in Semiconductors
Electrons and holes can be considered as quasi-classical particles with effective mass m*
In the presence of an electric field E, carriers move with average drift velocity vd = mE , m is the carrier mobility
  Mobility decreases with the increasing total concentration of ionized dopants
  Mobility is dependent on temperature
    decreases with increasing T if lattice scattering is dominant
    decreases with decreasing T if impurity scattering is dominant
The conductivity and the resistivity of a semiconductor is dependent on its mobile charge carrier concentrations and mobilities

## Slide 26: Diffusion
Particles diffuse from regions of higher concentration to regions of lower concentration region, due to random thermal motion.
26

## Slide 27: 1-D Diffusion Example
Thermal motion causes particles to move into an adjacent compartment every t seconds
  Each particle has an equal probability of jumping to the left or jumping to the right.
27

## Slide 28: Diffusion Current
D is the diffusion constant, or diffusivity.
28

## Slide 29: Total Current
29

## Slide 30: Non-Uniformly-Doped Semiconductor
The position of EF relative to the band edges is determined by the carrier concentrations, which is determined by the net dopant concentration.
In equilibrium EF is constant; therefore, the band-edge energies vary with position in a non-uniformly doped semiconductor:
30
Ev(x)
Ec(x)
EF

## Slide 31: Potential Difference due to n(x), p(x)
The ratio of carrier densities at two points depends exponentially on the potential difference between these points:
31

## Slide 32: Built-In Electric Field due to n(x), p(x)
Consider a piece of a non-uniformly doped semiconductor:
Ev(x)
Ec(x)
EF
32

## Slide 33: Einstein Relationship between D, m
In equilibrium there is no net flow of electrons or holes
 The drift and diffusion current components must balance each other exactly. (A built-in electric field exists, such that the drift current exactly cancels out the diffusion current due to the concentration gradient.)
Jn = 0 and Jp = 0
33
The Einstein relationship is valid for a non-degenerate semiconductor, even under non-equilibrium conditions.

## Slide 34: Example: Diffusion Constant
What is the hole diffusion constant in a sample of silicon with p = 410 cm2 / V s ?
Answer:
Remember: kT/q = 26 mV at room temperature.
34

## Slide 35: Quasi-Neutrality Approximation
If the dopant concentration profile varies gradually with position, then the majority-carrier concentration distribution does not differ much from the dopant concentration distribution.
  n-type material:
  p-type material:
  in n-type material
35

## Slide 36: Generation and Recombination
Generation:
Recombination:
Generation and recombination processes act to change the carrier concentrations, and thereby indirectly affect current flow
36

## Slide 37: Generation Processes
Band-to-Band
R-G Center
Impact Ionization
37

## Slide 38: Recombination Processes
Direct
R-G Center
Auger
Recombination in Si is primarily via R-G centers
38

## Slide 39: Direct vs. Indirect Band Gap Materials
Little change in momentum
is required for recombination
momentum is conserved by
photon emission
Large change in momentum
is required for recombination
momentum is conserved by
phonon + photon emission
Energy (E) vs. momentum (k) Diagrams
39
Direct:
Indirect:

## Slide 40: Excess Carrier Concentrations
Charge neutrality condition:
equilibrium values
40

## Slide 41: Low-Level Injection
Often the disturbance from equilibrium is small, such that the majority-carrier concentration is not affected significantly:
  For an n-type material:
  For a p-type material:
  However, the minority carrier concentration can be significantly affected.
41

## Slide 42: Indirect Recombination Rate
Suppose excess carriers are introduced into an n-type Si sample (e.g. by temporarily shining light onto it) at time t = 0.
How does p vary with time t > 0?
Consider the rate of hole recombination via traps:
Under low-level injection conditions, the hole generation rate is not significantly affected:
42

## Slide 43
The net rate of change in p is therefore
43

## Slide 44: Minority Carrier (Recombination) Lifetime
The minority carrier lifetime  is the average time an excess minority carrier “survives” in a sea of majority carriers
 ranges from 1 ns to 1 ms in Si and depends on the density of metallic impurities (contaminants) such as Au and Pt, and the density of crystalline defects. These impurities/defects give rise to localized energy states deep within the band gap. Such deep traps capture electrons or holes to facilitate recombination and are called recombination-generation centers.
44

## Slide 45: Relaxation to Equilibrium State
for electrons in p-type material
for holes in n-type material
Consider a semiconductor with no current flow in which thermal equilibrium is disturbed by the sudden creation of excess holes and electrons. The system will relax back to the equilibrium state via the R-G mechanism:
45

## Slide 46: Example: Photoconductor
Consider a sample of Si doped with 1016 cm-3 boron,
with recombination lifetime 1 s. It is exposed continuously to light, such that electron-hole pairs are generated throughout the sample at the rate of 1020 per cm3 per second, i.e. the generation rate GL = 1020/cm3/s
What are p0 and n0 ?
What are n and p ?
(Hint: In steady-state, generation rate equals recombination rate.)
46

## Slide 47
What are p and n ?
What is the np product ?
Note: The np product can be very different from ni2.
47

## Slide 48: Net Recombination Rate (General Case)
For arbitrary injection levels, the net rate of carrier recombination is:
48

## Slide 49: Summary
Electron/hole concentration gradient  diffusion
Current flowing in a semiconductor is comprised of drift and diffusion components for electrons and holes
  In equilibrium Jn = Jn,drift + Jn,diff = 0 and Jp = Jp,drift + Jp,diff = 0
The characteristic constants of drift and diffusion are related:
J = Jn,drift + Jn,diff + Jp,drift + Jp,diff
49

## Slide 50: Summary (cont’d)
Generation and recombination (R-G) processes affect carrier concentrations as a function of time, and thereby current flow
  Generation rate is enhanced by deep (near midgap) states due to defects or impurities, and also by high electric field
  Recombination in Si is primarily via R-G centers
The characteristic constant for (indirect) R-G is the minority carrier lifetime:
Generally, the net recombination rate is proportional to
50
p
n

## Slide 51: Problem on Electron Mobility